Twin index

---
A few preliminary definitions
Twofold twins are twins where only twin elements of order 2 exist (twofold twin axes, twin planes, twin inversion centers)
  - First-degree twofold twins or binary twins are twins where only one twin element of order 2 exists
  - higher-degree twofold twins are twins where more than one twin element of order 2 exist
Manifold twins are twins where ate least one twin element of order higher than 2 exists
  - First-degree manifold twins are twins where only one twin element of order higher than 2 exists
  - higher-degree manifold twins are twins where more than one twin element exist, of which at least one has order higher than 3

---
Twin index for twofold twins
The twin index is the number of lattice nodes restored or quasi-restored by the twin operation
The (quasi)-restored nodes define a lattice, the twin lattice.
(Quasi)-restored nodes define the cell based on the pair of elements (plane/direction) defining the cell of the twin lattice
The twin lattice either coincides with the lattice of the individual (twinning by merohedry) or is a sublattice of it (twinning be reticular merohedry/polyholohedry)
In the following, we talk about twofold twins unless differently specified

---
(210)
O
M
[210]
Only nodes at the corners of the red cell are restored.
There are N = 5 planes of the family (210) from O to M.
The twin index is n = 5 (n = N)
a
b

---
(310)
O
M
[310]
The nodes at the corners of the red cell and the node at the center are restored
There are N = 10 planes of the family (310) between O and M.
The twin index is n = 5 (n = N/2)
a
b

---
c
h+k odd:
Planes (100) et (010)
b
a
Switching from P to C cell has no effect on the density of nodes on
each plane but halves the interplanar distance

---
h+k odd:
Planes (210)
Switching from P to C cell has no effect on the density of nodes on
each plane but halves the interplanar distance
a
b
c

---
h+k even:
Planes (110)
Switching from P to C cell doubles the density of nodes on each plane but has no effect on the interplanar distance
a
b
c

---
A few definitions
(hkl) and [uvw] are the lattice plane and lattice row defining the cell of the twin lattice
O and M are successive lattice nodes along [uvw]
N = number of lattice planes of the family (hkl) from O to M
X = |hu+kv+lw|
n = twin index
Lind is the lattice of the individual
LT is the twin lattice
For twofold twins, the two-dimensional coincidence index is either 1 or 0
Let f be the number of lattice planes of the (hkl) family between O and M whose two dimensional coincidence index is 0
The twin index twofolds twins is simply n = X/f

---
h+k odd; u+v odd
(210)
O
M
[210]
P type Lind: N = n = X = 5, the cell of LT is primitive
C type Lind: N = 2X= 10, n = N/2 = X = 5, the cell of LT is C-centered
a
b

---
h+k odd; u+v even
(210)
O
M
M
[110]
P type Lind: N = n = X= 3, the cell of LT is primitive
C type Lind: N = n = X = 3, the cell of LT is primitive and
is twice smaller that that of P type Lind
a
b

---
h+k even; u+v odd
(110)
O
M
[210]
P type Lind: N = n = X = 3, the cell of LT is primitive
C type Lind: N = n = X = 3, the cell of LT is primitive and
is twice smaller that that of P type Lind
a
b

---
h+k even; u+v even
O
(310)
M
M
[310]
P type Lind: N = X = 10, n = X/2 = 5; the cell of LT is C-centered
C type Lind: N = n = X/2 = 5, the cell of LT is primitive and
is twice smaller that that of P type Lind
a
b

---
Summarizing....
Computation of the twin index for twofold twins
N = number of lattice planes of the family (hkl) between two successive lattice nodes along [uvw]
n = twin index

---
Primitive cell
C-centered cell

---
B-centered cell
A-centered cell

---
cC
cI
I-centered cell
from a C-centered cell
aC
bC
bI
aI

---
F-centered cell
F and I lattice types are one the dual of the other. The conditions for an I-centered cell apply also to an F-centered cell provided that (hkl) and [uvw] are exchanged.

---
Example of different centering in Lind and LT
O
(310)
M
[310]
The cell of Lind is I
The cell of LT is S -
before any possible transformation
1/2
1/2
1/2
1/2
1/2
1/2
1/2
1/2
1/2
1/2
1/2
1/2
1/2
1/2
1/2
1/2
a
b

---
(011) twin in cassiterite (SnO2) and rutile (TiO2)

---
cind
[012]ind
bT
cT
M
O
bind
[011]ind

---
(031) twin in chrysoberyl BeAl2O4

---
cind
cT
[023]ind
bT
M
O
bind
cind
cind
cT
cT
[023]ind
[023]ind
bT
bT
M
M
O
O
bind
bind
[013]ind
[013]ind
[013]ind

---
What about manifold twins?
Greek-cross fourfold-twin in staurolite
C2/m
a = 7.871 Å
b = 16.620 Å
c = 5.656 Å
 = 90º
Twin operation: 4[100]
[100] is perpendicular to (100)
X = |1·1 + 0·0 + 0·0|
Is the twin index 1?

---
c
b''
12 nodes in the tC cell of LT: the twin index is 6
tC is not a standard cell – let us transform it to the standard tP cell
b'
6 nodes in the tP cell of LT: the twin index is 6
a'
no nodes at all restored on this plane
2 nodes out of 6 restored on this plane (restoration index is 3)
a''
b
1 plane of the (100) family out of 2 has a coincidence index of 3
a
c'
c''
n = 2·3 / 1 = 6

---
How to compute the twin index of a manifold twin?
Let N be the number of lattice planes of the (hkl) family passing within the cell of the twin lattice
Out of these N planes,  be the number of planes that are partially restored by the twin operation (the other N- are not restored at all.
Let  be the reciprocal of the two-dimensional coincidence index for a plane of the (hkl) family that is partially restored by the twin operation
The twin index is n = NX/x
Cumbersome? Than take a shorter route:
Find a twofold operation in the same coset and apply the classical formula!